2010 Final Report – Nano-Oxide Photocatalysis for Solar Energy Conversion
 Page 8
2011 Final Report – Nano-Oxide Photocatalysis for Solar Energy Conversion
 Page  1

	Nano-Oxide Photocatalysis for Solar Energy Conversion

DE-FG02-07ER46418

Frederick Seitz Materials Research Laboratory
University of Illinois at Urbana-Champaign


Cluster Participants:
James N. Eckstein

Kenneth S. Suslick (Cluster Leader)

Graduate Student Researchers:
Maria Fortunato (25%)
Richard Helmich (50%)

Brian Mulcahy (50%)

Primary National Laboratory Collaborators:
Anand Bhatacharya (ANL)

Ivan Bozovic (BNL)
Research Accomplishments
· We have very recently discovered a new hydrogen-producing photocatalyst is BiNbO4 (Figure 1). BiNbO4 powders prepared by solid state reaction were tested for photocatalytic activity in methanol solutions under UV irradiation. When the material is tested without the presence of a Pt co-catalyst, photocatalytic activity for H2 evolution is superior to that of TiO2. It was also found that BiNbO4 photodegrades into metallic Bi and reduced Nb oxides after use; materials were characterized by SEM, XRD, and XPS. Adding Pt to the surface of the photocatalyst increases photocatalytic activity and importantly, helps to prevent photodegradation of the oxide material. With 1 wt. % Pt loading, photodegradation is essentially absent. BiNbO4 photodegrades into metallic Bi and reduced Nb oxides after use; materials were characterized by SEM, XRD, and XPS. Adding Pt to the surface of the photocatalyst increases photocatalytic activity and importantly, helps to prevent photodegradation of the oxide material. With 1 wt. % Pt loading, photodegradation is essentially absent.

[image: image1.emf]0 1 2 3 4 5

0

200

400

600

800

1000

1200

1400

1600

1800

H

2

Evolved (

µ

mol)

Time of Irradiation (hr.)

a

c

b

0 1 2 3 4 5

0

200

400

600

800

1000

1200

1400

1600

1800

H

2

Evolved (

µ

mol)

Time of Irradiation (hr.)

0 1 2 3 4 5

0

200

400

600

800

1000

1200

1400

1600

1800

H

2

Evolved (

µ

mol)

Time of Irradiation (hr.)

a

c

b


Figure 1. The amount of H2 evolved over time for BiNbO4 (a) without a co-catalyst, (b) with 0.2 wt.% Pt nanoparticles, and (c) with 1.0 wt.% Pt.

[image: image2.jpg]



Figure 2. SEM micrographs of BiNbO4 photocatalysts (A) before use, (B) after use without a co-catalyst, (C) with 0.2 wt.% Pt, and (D) with 1.0 wt.% Pt.  Higher magnification images of delaminated particles found in samples after use (E) without a co-catalyst and (F) with 0.2 wt.% Pt.
· We have investigated BiVO4 as a new visible-light photocatalyst for O2 evolution, the other half of the photocatalytic splitting of water. We have prepared BiVO4 powders with unique particle architectures using USP. Gases created from the evaporation of solvent and the decomposition of precursor materials shape the morphology of the particles as the solids are formed in the heated aerosol. The BiVO4 powder was tested as an oxygen evolving photocatalyst by monitoring the kinetics of O2 formation from an aqueous AgNO3 solution irradiated with ( > 400 nm light. USP prepared BiVO4 was found to have significantly superior photocatalytic activity compared to commercial BiVO4 and WO3 (which is the standard O2 generating photocatalyst in the field), likely due to differences in particle morphology. 
· We also discovered a very simple route to nanostructured carbon materials, produced from simple precursors such as sucrose and sodium carbonate or bicarbonate using a facile, one-step USP process without the need for sacrificial templates. The high surface areas and unique hierarchical pore structures of these materials suggest that they may find use as adsorbents and catalyst supports. The hollow interior (Figure 3) provides a low-density, free-flowing microsphere morphology that may prove especially useful for any applications requiring a fluidized bed reactor or packed chromatographic column.
[image: image3.emf]
Figure 3. TEM images of carbons prepared by ultrasonic spray pyrolysis from 0.5Msucrose and (A) 1.0MNa2CO3, (B) 0.5MNa2CO3, (C) 0.1M Na2CO3, (D) 1.0 M NaHCO3, (E) 0.5 M NaHCO3, and (F) 0.1 M NaHCO3. Furnace residence time is 9 s at 800 _C.
· A novel and facile synthetic approach to prepare hierarchically nanostructured titanium nitride via an in situ dual templating was developed using USP. No pre-structured templates are necessary to produce the hierarchical nanostructures; instead, a template is generated in situ during the synthesis from a liquid core and the resulting spherical shell, and the template is removed in the final heating without any additional chemical etching.

	[image: image4.wmf] 

 


	[image: image5.wmf]Liquid

droplet

ZnO

formation

TiO

2

formation

& interparticle 

rxn

Hollow Zn

2

TiO

4

sphere

Liquid

droplet

ZnO

formation

TiO

2

formation

& interparticle 

rxn

Hollow Zn

2

TiO

4

sphere

[image: image6.wmf]liquid

droplet

liquid

droplet

solid TiO

2

sphere

solid

TiN

sphere

hollow Zn

2

TiO

4

sphere

mesoporous 

TiN

hollow sphere

900 

°

C

air

1000 

°

C

NH

3

900 

°

C

air

Zn 

↑

NH

3

1000 

°

C

a

b

aq. 

Ti

IV

aq. 

Ti

IV

+ Zn

+2

liquid

droplet

liquid

droplet

solid TiO

2

sphere

solid

TiN

sphere

hollow Zn

2

TiO

4

sphere

mesoporous 

TiN

hollow sphere

900 

°

C

air

1000 

°

C

NH

3

900 

°

C

air

Zn 

↑

NH

3

1000 

°

C

a

b

liquid

droplet

liquid

droplet

solid TiO

2

sphere

solid

TiN

sphere

hollow Zn

2

TiO

4

sphere

mesoporous 

TiN

hollow sphere

900 

°

C

air

1000 

°

C

NH

3

900 

°

C

air

Zn 

↑

NH

3

1000 

°

C

a

b

aq. 

Ti

IV

aq. 

Ti

IV

+ Zn

+2




· [image: image7.png]NORMAL

INVERTED

AlO,(-

TiO,

TiO,

Lag 1Srp O

TiO,

Lag 1Srp O

TiO,

SrO

TiO,

SrO

SrO

TiO,

SrO

TiO,

TiO

TiO,

SrO

SrO

TiO,

TiO,

SrO

SrO

STO
STO
LTO
LAO
LAO



Interfaces between two band insulators.  Work continued on how to make two dimensional electron systems in oxides. Last year we began a systematic study of inverted LaAlO3 (LAO) to SrTiO3 (STO) interfaces. Instead of preparing a Ti terminated STO substrate and then growing an LAO film on top, our idea was to grow STO on top of LAO. This would effectively solve the problem of contacting the 2DEG which is difficult in the case of LAO on STO since LAO is much more insulating than STO. The charge transfer discontinuity that is thought to give rise to the 2DEG has to be explicitly grown in this case. The architectures grown [image: image8.png]time 2000

1500

AyisualulJeinoads




are shown schematically in Figure 4. On top of a substrate, typically STO, we grow a layer of LAO. In Figure 4 this is shown to be only 2 unit cells thick, but often it was substantially thicker. Then to transition to the STO something else must be done. In order to get an electron gas it is necessary to have the same atomic oxide layer structure sequence that is in the “normal” layer. Since layers grown always terminate in the transition metal oxide, to get the same atomic oxide layering it is necessary to grow an interfacial layer of LaTiO3. This requires a very different oxygen environment than either STO or LAO do.

[image: image9.png]



The layers grown typically showed good crystalline order during growth as evidenced by strong specular RHEED reflections and layer by layer growth as evidenced by spontaneous and self generated oscillations of the RHEED specular intensity. These are shown in Figure 5. Figure 6 shows a cross sectional TEM lattice image taken by students of J-M Zuo in which good crystalline order of the heterostructure can be seen. In transport we continued to observe low temperature anomalies similar to those reported last year. With improved epitaxy we are able to report improved magneto transport results. We obtained a room temperature mobility  of 3.7 cm2/Vsec and a sheet carrier density of 5.3x1014 cm-2. The later number is very close to the value expected for doping via the polarization catastrophe that was originally proposed, but hardly ever reported. Coupled with the good mobility number (good for STO) this may indicate we are producing more ideal 2DEGs. We are interested in continuing this work to determine the properties exhibited by these new materials.

Publications - 2009-Present (Cluster PI)
1. J.H. Bang, S.H. Lim, E. Park, and K.S. Suslick, “Dual Templating Synthesis of Mesoporous Titanium Nitride Microspheres”, Advanced Materials, 21, 1-5 (2009).

2. S.S. Dunkle and K.S. Suslick, “Photodegradation of BiNbO4 Powder during Photocatalytic Reactions”, J. Phys. Chem. C, 113, 10341-10345 (2009).
3. S.S. Dunkle, R.J. Helmich, and K.S. Suslick, “BiVO4 as a Visible-Light Photocatalyst Prepared by Ultrasonic Spray Pyrolysis”, J. Phys. Chem. C, 113, 11980-11983 (2009).

4. J.H. Bang and K.S. Suslick, “Applications of Ultrasound to the Synthesis of Nanostructured Materials”, Advanced Materials, 22, 1039–1059 (2010).

5. H.X. Xu and K.S. Suslick, “Water-Soluble Fluorescent Silver Nanoclusters”, Advanced Materials, 22, 1078-1082 (2010).

6. M.E. Fortunato, M. Rostam-Abadi, and K.S. Suslick, “Nanostructured Carbons Prepared by Ultrasonic Spray Pyrolysis”, Chem. Matl., 22, 1610–1612 (2010).
7. X. Zhai, C.S. Mohapatra, A.B. Shah, J.-M. Zuo, and J.N. Eckstein, “New optical absorption bands in atomic-layer superlattices”, Advanced Materials, 22, 1136-1139 (2010).

Patents - 2009-Present (filed)

James Eckstein

None
Kenneth Suslick

None
Awards – 2009-Present
James Eckstein

None
Kenneth Suslick

· Materials Research Society Fellow (2009)

· Acoustic Society of America Mentor Award (2009)

· 3ème Cycle Lectureship, Switzerland (2010)
· Fellow, Guggenheim Memorial Foundation (2011) 
· Fellow, American Chemical Society (2010) 
Invited Talks – 2009-present
1. J.N. Eckstein, 2nd International Workshop, Nanoxide - Oxide Interfaces, “New phases and optical transitions at oxide heterostructures”, Valbella Grissons, Switzerland (April, 2009).
2. J.N. Eckstein, Novel Electronics Materials Summer School, “Electronic Oxides”, Ameland, Netherlands (June, 2009).

3. K.S. Suslick, California Institute of Technology, "Colorimetric Sensor Arrays: An Adventure in Molecular Recognition", Pasadena, CA (February, 2009).
4. K.S. Suslick, University of California, Riverside, "Colorimetric Sensor Arrays: An Adventure in Molecular Recognition", Riverside, CA (February, 2009).
5. K.S. Suslick, New Sensors for Environmental Monitoring, Pittsburgh Conference (PittCon), Chicago, IL (March, 2009).

6. K.S. Suslick, MRS National Meeting, “Photocatalysis with metal oxides”, San Francisco, CA (April, 2009).
7. K.S. Suslick, Workshop on New Sensor Technology, Solvay Corporation, Brussels, Belgium (June, 2009).

8. K.S. Suslick, Plenary Lecturer, Beijing Conference and Exhibition on Instrumental Analysis (BCEIA ’09), "Colorimetric Sensor Arrays: An Adventure in Molecular Recognition", Beijing (November, 2009).

9. K.S. Suslick, Department of Chemistry, Peking University, “Sonochemistry”, Beijing (November, 2009).

10. K.S. Suslick, Department of Chemistry, Tsinghua University, “The Chemical Effects of Ultrasound”, Beijing (November, 2009).

11. K.S. Suslick, Department of Chemistry, University of North Texas, Denton “Sonochemistry”, (March, 2010).

12. K.S. Suslick, Department of Chemistry, University of California, Davis, "Colorimetric Sensor Arrays: An Adventure in Molecular Recognition", (March, 2010).

13. K.S. Suslick, 3ème Cycle Lectures:  Universities of Fribourg, Neuchatel, Geneva, and Bern. (April 2010)
14. K.S. Suslick, “Ultrasonic effects on crystallization” Invited Speaker, 2010 Association for Crystallization Technology Meeting, New Brunswick, NJ. (May 2010)
15. K.S. Suslick, “Conditions created during Cavitation”, Plenary Lecturer, 12th Meeting of the European Sonochemistry Society, Chania, Crete. (June 2010)
16. K.S. Suslick, Invited Speaker, Sonochemistry Symp., Pacifichem 2010, Honolulu. (Dec. 2010)
17. K.S. Suslick, Schwinger Foundation Symposium on Spontaneous Energy Focusing Phenomena, NTU, Singapore. (Aug. 2010)
18. K.S. Suslick, “The Optoelectronic Nose”, Invited Speaker, Targeting Chem. & Biol. Warfare Agents Symposium, Pacifichem 2010, Honolulu. (Dec., 2010)
19. K.S. Suslick, Provost’s Visiting Scholars & Artists Program, Western Michigan U. (May 2011)
20. K.S. Suslick, Invited Speaker, Materials & Molecular Design & Discovery Initiative, Argonne National Laboratory. (June 2011)
21. K.S. Suslick, “Conditions during Cavitation” Invited Speaker, Nonlinear Acoustics Symposium, Acoustical Society of America National Meeting, Seattle. (Aug. 2011)
22. K.S. Suslick, “The Optoelectronic Nose”, Invited Speaker, Gordon Research Conference on Detecting Illicit Substances, Lucca, Italy (Aug., 2011).

23. K.S. Suslick, Invited Speaker and symposium organizer, “The Optoelectronic Nose”, Intl. Symp. on Olfaction & Electronic Noses (ISOEN-2011), NYC. (Sept 2011)
DOE Collaborators
James Eckstein

Anand Bhattacharya, Argonne National Laboratory

Ivan Bozovic, Brookhaven National Laboratory
Kenneth Suslick
None

Nano-Oxide Photocatalysis for Solar Energy Conversion: Unexpended funds
No unexpended funds remain.
	Current and Pending Support

	Investigator: James N. Eckstein

	Support:
	 FORMCHECKBOX 
 Current 
	 FORMCHECKBOX 
 Pending 
	 FORMCHECKBOX 
 Submission Planned in Near Future 

	Project/Proposal Title: Quantum Materials at the Nanoscale (11 Investigators)

	Source of Support: Department of Energy

	Total Award Amount (Investigator): $307,101
	Total Award Period Covered: 08/01/07 – 07/31/10

	Total Award Amount: $5,145,000

Location of Project:  University of Illinois at Urbana-Champaign

	Person-Months Per Year Committed to the Project.
	Cal: 
	Acad: 
	Sumr:  0.50

	Support:
	 FORMCHECKBOX 
 Current 
	 FORMCHECKBOX 
 Pending 
	 FORMCHECKBOX 
 Submission Planned in Near Future 

	Project/Proposal Title: Nano-Oxide Photocatalysis for Solar Energy Conversion

No overlap with Quantum Materials at the Nanoscale Cluster.

	Source of Support: Department of Energy

	Total Award Amount (Investigator):  $337,257
	Total Award Period Covered: 08/01/07 – 07/31/10

	Total Award Amount: $750,000

Location of Project:  University of Illinois at Urbana-Champaign

	Person-Months Per Year Committed to the Project.
	Cal: 
	Acad: 
	Sumr:  0.50

	Support:
	 FORMCHECKBOX 
 Current 
	 FORMCHECKBOX 
 Pending 
	 FORMCHECKBOX 
 Submission Planned in Near Future 

	Project/Proposal Title: Digital Synthesis A Novel Pathway to New Collective States in the Complex Oxides

No overlap with Quantum Materials at the Nanoscale Cluster.

	Source of Support:  Argonne National Laboratory/Department of Energy

	Total Award Amount:  $423,152
	Total Award Period Covered: 01/01/07 – 08/31/10

	Location of Project:  University of Illinois at Urbana-Champaign

	Person-Months Per Year Committed to the Project.
	Cal: 
	Acad: 
	Sumr:  0.50

	Support:
	 FORMCHECKBOX 
 Current 
	 FORMCHECKBOX 
 Pending 
	 FORMCHECKBOX 
 Submission Planned in Near Future 

	Project/Proposal Title: Center for Emergent Superconductivity (10 Illinois Investigators)

No overlap with Quantum Materials at the Nanoscale Cluster.

	Source of Support:  Brookhaven National Laboratory (DOE/EFRC)

	Total Award Amount (Investigator): $806,450 
	Total Award Period Covered: 08/14/09 – 08/13/14

	Total Award Amount (Illinois): $6,216,000

Location of Project:  University of Illinois at Urbana-Champaign

	Person-Months Per Year Committed to the Project.
	Cal: 
	Acad: 
	Sumr:  0.50

	Support:
	 FORMCHECKBOX 
 Current 
	 FORMCHECKBOX 
 Pending 
	 FORMCHECKBOX 
 Submission Planned in Near Future 

	Project/Proposal Title: Reduction of Decoherence in Flux Qubits

No overlap with Quantum Materials at the Nanoscale Cluster.

	Source of Support: University of California, Berkeley (USARO Prime)

Total Award Amount (Investigator): $2,000,000

	Total Award Amount:  $4,001,945
	Total Award Period Covered: 06/15/09 – 04/30/14

	Location of Project:  University of Illinois at Urbana-Champaign

	Person-Months Per Year Committed to the Project.
	Cal: 
	Acad: 
	Sumr:  1.00


	Support:
	 FORMCHECKBOX 
 Current 
	 FORMCHECKBOX 
 Pending 
	 FORMCHECKBOX 
 Submission Planned in Near Future 

	Project/Proposal Title: Quantum Materials at the Nanoscale (12 Investigators)

	Source of Support: Department of Energy

	Total Award Amount:  $5,400,000
	Total Award Period Covered: 08/01/10 – 07/31/13

	Location of Project:  University of Illinois at Urbana-Champaign

	Person-Months Per Year Committed to the Project.
	Cal: 
	Acad: 
	Sumr:  0.50


	Current and Pending Support

	Investigator: Kenneth S. Suslick

	Support:
	 FORMCHECKBOX 
 Current 
	 FORMCHECKBOX 
 Pending 
	 FORMCHECKBOX 
 Submission Planned in Near Future 

	Project/Proposal Title: Nano-Oxide Photocatalysis for Solar Energy Conversion, (multi-PI award Seitz Materials Lab, UIUC)
Project Focus: The goal of this project is to develop new hierarchical assemblies of nanostructured metal oxides for potential use in photochemical water splitting.

	Source of Support:  Department of Energy/BES

	Total Award Amount:  $415,000
	Total Award Period Covered: 08/01/07 – 07/31/11

	Location of Project:  University of Illinois at Urbana-Champaign

	Person-Months Per Year Committed to the Project.
	Cal: 
	Acad: 
	Sumr:  1.00

	Support:
	 FORMCHECKBOX 
 Current 
	 FORMCHECKBOX 
 Pending 
	 FORMCHECKBOX 
 Submission Planned in Near Future 

	Project/Proposal Title:  A VOC Dosimeter Based On A Colorimetric Sensor Array

RFA-ES-06-011:   U01ES16011-01

	Project Focus: Use of colorimetric sensor arrays as environmental sensors of volatile organic compounds for personal exposure assessment.

	Source of Support:  NIH

	Total Award Amount: $2,306,718
	Total Award Period Covered: 07/01/07 – 06/30/11

	Location of Project: University of Illinois at Urbana-Champaign

	Person-Months Per Year Committed to the Project.
	Cal:     
	Acad:     
	Sumr:  1

	Support:
	 FORMCHECKBOX 
 Current 
	 FORMCHECKBOX 
 Pending 
	 FORMCHECKBOX 
 Submission Planned in Near Future 

	Project/Proposal Title: New Synthetic Methodologies for Nanostructured Materials Using Ultrasound

	Project Focus: The goal of this project is the exploration of synthetic applications of sonochemistry and of ultrasonic spray pyrolysis to nanostructured inorganic materials. This proposal is strictly oriented towards the synthesis, preparation, and characterization of novel materials. 

	Source of Support:  National Science Foundation, Division of Materials Research

	Total Award Amount:  $340,000
	Total Award Period Covered: 09/01/09 – 8/30/12

	Location of Project:  University of Illinois at Urbana-Champaign

	Person-Months Per Year Committed to the Project.
	Cal:     
	Acad: 
	Sumr:  0.75

	Support:
	 FORMCHECKBOX 
 Current 
	 FORMCHECKBOX 
 Pending 
	 FORMCHECKBOX 
 Submission Planned in Near Future 

	Project/Proposal Title: The Chemical Effects of High Intensity Ultrasound: Sonoluminescence  

Competing Renewal of NSF CHE 0315494 (Suslick)

	Project Focus: The goal of this project is to investigate sonoluminescence as a spectroscopic probe of the conditions created during acoustic cavitation in liquids.

	Source of Support:  National Science Foundation, Division of Chemistry

	Total Award Amount:  $ 521,845
	Total Award Period Covered: 06/01/10 – 05/30/14

	Location of Project:  University of Illinois at Urbana-Champaign

	Person-Months Per Year Committed to the Project.
	Cal:     
	Acad: 
	Sumr:  0.75

	Support:
	 FORMCHECKBOX 
 Current 
	 FORMCHECKBOX 
 Pending 
	 FORMCHECKBOX 
 Submission Planned in Near Future 

	Project/Proposal Title: Applications of Ultrasound to Lignocellulosic Biofuel Production

	Project Focus: The goal of this project is to investigate applications of ultrasound to modification of lignocellulose.

	Source of Support:  Energy Biosciences Institute (UC Berkeley & UIUC)

	Total Award Amount:  $ 242,000
	Total Award Period Covered: 06/01/10 – 05/30/12

	Location of Project:  University of Illinois at Urbana-Champaign

	Person-Months Per Year Committed to the Project.
	Cal:     
	Acad: 
	Sumr:  0.75


Figure 4. Layer architecture for both the normal as well as the inverted LAO-STO heterointerface.





Figure 5. RHEED pattern observed during the growth of STO and oscillations of specular spot showing layer by layer growth.





Figure 6. Cross sectional TEM showing the well ordered LAO layer grown on top of the etched STO substrate.








Frederick Seitz Materials Research Laboratory – University of Illinois at Urbana-Champaign
Frederick Seitz Materials Research Laboratory – University of Illinois at Urbana-Champaign


