## Slide 1
Fabrication, Oxidation, and Combustion of Nanoscale Magnesium Diboride and Tetraboride
15th International Workshop on Combustion and Propulsion
July 6 – 9, 2025, Pescara, Italy
Andre Molina, Miguel Camarena, Juan Noveron, and Evgeny Shafirovich
The University of Texas at El Paso

## Slide 2: Motivation
One of the main approaches to improving ignition and combustion of boron particles is the addition of magnesium.
  Boron/magnesium mixtures and composites
  Magnesium borides
There exist borides with different B/Mg ratios (e.g., 2:1, 4:1, 7:1).
MgB2 has been studied extensively as a superconductor and as a fuel for propulsion systems.
Since the addition of Mg decreases the energy density, the feasibility to use magnesium borides with higher B/Mg ratios should be examined.
MgB4
MgB7
MgB2

## Slide 3: Objectives
To fabricate nanoscale MgB2 and MgB4 by combustion synthesis and by sintering in a tube furnace followed by high-energy ball milling and by acid leaching for oxide removal.
To study their oxidation by thermogravimetric analysis (TGA).
To study their combustion using laser ignition, high-speed video recording, and emission spectroscopy.

## Slide 4: Combustion Synthesis
Chemical oven
A ceramic (BN) crucible with an B/Mg pellet surrounded by an annular layer of a Ti/B (1:2 mole ratio) mixture
The crucible is placed into a chamber filled with Ar.
The Ti/B mixture is ignited by a hot wire or by a laser.
The released heat ignites the B/Mg mixture.
Heating rate: 300-500 K/s
Chemical oven schematic
Crucible
Ti/B mixture
B/Mg pellet
Laser ignition setup
Hot-wire ignition setup

## Slide 5: Sintering in a Tube Furnace
B/Mg pellet in Ar flow
Heated at 5 °C/min up to 650–1050°C.
Held for 1 – 6 h.
Cooled at a rate of 5 °C/min.
MTI GSL-1500x

## Slide 6: High-energy Ball Milling
Ball-powder mass ratio: 15 – 30
ZrO2 vials
ZrO2 balls (diameter: 0.5 – 12.7 mm)
Environment: Ar
Milling time: 1 – 4 h
SPEX 8000D Shaker Mill

## Slide 7: Thermogravimetric Analysis (TGA)
2 – 5 mg powder
Alumina crucibles (85 μL)
Temperature range: 25 – 1550 °C
Heating rate: 2 – 10 °C /min
Argon or oxygen flow (50 mL/min)
Netzsch STA 449 F3 Jupiter

## Slide 8: Combustion Experiments
Laser ignition
  Synrad Firestar ti-60
  Beam diameter: 2.0 ± 0.3 mm
  32 W, 100 ms
  Environment: O2
High-speed video camera
  Phantom v1210
  Nikon AF NIKKOR 60 mm f/2.8D
  3000 fps
Spectrometer
  AvaSpec-ULS2048CL-EVO-RS-UA
  Wavelength range: 200 – 1100 nm
  Sampling time: 1.35 ms
Sample holders

## Slide 9: XRD of Synthesized MgB2 and MgB4
At 2:1, both methods yield similar products.
At 4:1, the tube furnace forms MgB₄ + MgO, while the chemical oven also produces MgB₂.
MgO
MgO

## Slide 10: Purification of Synthesized Materials
Leaching with acetic acid and nitric acid removes oxides effectively.
MgO
MgO
MgO
MgO
Notes: We submerge the borides in dilute acid for 5 minutes, remove the acid with vacuum filtration, wash away residual acid away with ethanol and water
We cannot use identical solutions of acid for each phase, the borides become increasingly more acid insoluble with increasing boron content. For MgB2 we needed to use an anhydrous solution of 10% acetic acid in toluene, and for MgB4 we have a lot more options, and we can use HCl and HNO3.

## Slide 11: Decreasing Particle Size
Evolution of MgB2 and MgB4 XRD patterns during milling
MgB2 (milled)
MgB2
MgB4 (milled)
MgB4
After 4 hours of milling, peak broadening indicates a reduced crystallite size.

## Slide 12: Decreasing Particle Size
High-energy ball milling has produced nanoscale MgB2 and MgB4.
MgB2
MgB4

## Slide 13: Decomposition of MgB₂ and MgB₄
MgB2 decomposes into MgB4 + Mg
MgB4 decomposes into MgB7 + Mg
MgB7 decomposes into MgB20 + Mg
Decomposition of MgB2 is a multi-step process known from prior studies.
MgB4 is also a multi-step process.

## Slide 14: Oxidation of MgB₂ and MgB₄
MgB4 Max mass = 266%
MgB2 Max mass = 239%
B Max mass = 322%
Extent of conversion
Mg: 100%
B: 74%
MgB2: 93%
MgB4: 95%
MgB2 (milled): 90%
MgB4 (milled): 87%
Both borides exhibit high extents of conversion compared to boron.
MgB4 is oxidized at a much lower temperature than MgB2.

## Slide 15: Combustion of MgB₂ and MgB₄
Video of combustion propagation (slowed 12x)
Mg
B
MgB2
MgB2
(milled)
MgB4
(milled)
MgB4

## Slide 16: Combustion of MgB₂ and MgB₄
Images of combustion propagation.
Time zero is the onset of light emission.
Mg
B
MgB2
MgB2
(milled)
MgB4
(milled)
MgB4

## Slide 17: Linear Burn Rates of MgB₂ and MgB₄
Chart: Burn Rate (mm/s)
| Mg | B | MgB2 (milled) | MgB4 (milled) | 2-1 B/Mg Mix | 4-1 B/Mg Mix
 | 1010.2263 | 91.3986 | 762.3024 | 489.1969
Both MgB2 and MgB4 burn much faster than B.
MgB4 burns slower than MgB2.
1010
91
489
762

## Slide 18: BO2 Emission Profile
Sample | Duration (s)*
B | 1.71
MgB2 | 0.77
MgB4 | 1.81
MgB2 (milled) | 1.26
MgB4 (milled) | 1.60
Onset
End
*Average values
MgB2 shows a shorter BO2 emission time.

## Slide 19: Emission Spectra of MgB₂ and MgB4
MgB4 emission spectra over time
MgO
BO2
Na, K, Li
MgB4 spectrum has much lower MgO peaks.
MgB2 emission spectra over time

## Slide 20: Conclusions
Fabrication
  Synthesis in a tube furnace produced MgB4 without MgB2 additive.
  Nanoscale MgB2 and MgB₄ have been obtained by using high-energy ball milling.
  Leaching with acetic acid and nitric acid is an effective means to remove oxides.
Oxidation
  Both borides exhibit high extents of conversion compared to boron.
  MgB4 is oxidized at a lower temperature than MgB2.
Combustion
  MgB2 and MgB4 burn much faster than B.
  MgB4 burns slower than MgB2.

## Slide 21
Acknowledgment
This material is based upon work supported by the U.S. Department of Energy’s Office of Energy Efficiency and Renewable Energy (EERE) under the award number DE-EE0010429.
Disclaimer
This report was prepared as an account of work sponsored by an agency of the United States Government. Neither the United States Government nor any agency thereof, nor any of their employees, makes any warranty, express or implied, or assumes any legal liability or responsibility for the accuracy, completeness, or usefulness of any information, apparatus, product, or process disclosed, or represents that its use would not infringe privately owned rights. Reference herein to any specific commercial product, process, or service by trade name, trademark, manufacturer, or otherwise does not necessarily constitute or imply its endorsement, recommendation, or favoring by the United States Government or any agency thereof. The views and opinions of authors expressed herein do not necessarily state or reflect those of the United States Government or any agency thereof.