## Slide 1
AMR Project ID # ST250
This presentation does not contain any proprietary, confidential, or otherwise restricted information
DOE Hydrogen Program
2024 Annual Merit Review and Peer Evaluation Meeting
May 6 – 9, 2024
Principal Investigator: Evgeny Shafirovich
Students: Andre Molina (PhD Research Associate)
Miguel Camarena (Graduate Research Assistant)
Organization: The University of Texas at El Paso
DOE project award #: DE-EE0010429
Combustion Synthesis of Nanoscale Magnesium Borides with Improved Hydrogen Uptake and Release

## Slide 2
Acknowledgment
This material is based upon work supported by the U.S. Department of Energy’s Office of Energy Efficiency and Renewable Energy (EERE) under the award number DE-EE0010429.
Disclaimer
This report was prepared as an account of work sponsored by an agency of the United States Government. Neither the United States Government nor any agency thereof, nor any of their employees, makes any warranty, express or implied, or assumes any legal liability or responsibility for the accuracy, completeness, or usefulness of any information, apparatus, product, or process disclosed, or represents that its use would not infringe privately owned rights. Reference herein to any specific commercial product, process, or service by trade name, trademark, manufacturer, or otherwise does not necessarily constitute or imply its endorsement, recommendation, or favoring by the United States Government or any agency thereof. The views and opinions of authors expressed herein do not necessarily state or reflect those of the United States Government or any agency thereof.

## Slide 3: Project Goal
Overarching Goal:
Develop high-capacity reversible metal hydrides that can be dehydrogenated and recharged at relatively low temperatures and pressures.
Specific Objectives:
Fabricate nanoscale magnesium boride powders with various B/Mg atomic ratios using self-propagating high-temperature synthesis (combustion synthesis).
Investigate the effects of B/Mg atomic ratio and particle size on the hydrogenation and dehydrogenation properties of the obtained magnesium borides.

## Slide 4
Particle size and B/Mg ratio affect the hydrogenation of magnesium borides.
Hydrogenation of nanoscale MgB0.75 (instead of MgB2) still needs 700 bar and 280°C.
(Y.-S. Liu et al., J. Phys Chem C 124 (2020) 21761)
The project aims to further decrease the required P and T via synthesis of nanoscale MgBx (x < 2 and x > 2) phases.
Project Start Date: 03/01/2023
Project End Date: 02/28/2025
Timeline
Barriers
Collaborator: Dr. Vitalie Stavila, Sandia National Laboratories – Livermore
Partners
Overview
Total Project Budget: $300,000
  DOE Share: $300,000
  Cost Share: 0
  DOE Funds Spent*: $137,771
* As of 03/01/2024
Budget

## Slide 5
Potential Impact
The project complements the research on reversible metal hydrides for hydrogen storage, conducted at the Hydrogen Materials – Advanced Research Consortium (HyMARC).
The HyMARC has been investigating magnesium borohydride, Mg(BH4)2, as the material is reversible and has a theoretical hydrogen content of 14.9 wt%.
Complete dehydrogenation of Mg(BH4)2 generates MgB2, which requires very high pressures and temperatures to regenerate the borohydride.
Particle size and B/Mg ratio affect the hydrogenation of magnesium borides.
  Hydrogenation of nanoscale MgB0.75 still needs 700 bar and 280°C.
The project aims to decrease the required P and T via synthesis of nanoscale MgBx (x < 2 and x > 2) phases.

## Slide 6
Approach
Synthesis of magnesium borides with various B/Mg atomic ratios by two methods:
  Combustion synthesis
  A tube furnace
Characterization of the obtained materials:
  X-ray diffraction analysis
  Scanning electron microscopy
  Laser diffraction particle size analysis
  Specific surface area analysis
Hydrogenation and dehydrogenation:
  Hydrogenation is first studied in a high-pressure differential scanning calorimeter (up to 150 bar).
  Next, hydrogenation and dehydrogenation are studied using pressure-composition-temperature measurements and high-pressure hydrogenation at SNL (up to 1000 bar and 450 °C).

## Slide 7
Approach: Safety Planning and Culture
This project was NOT required to submit a safety plan to the Hydrogen Safety Panel (HSP).
Prioritizing safety and analyzing hazards:
  The Operating Procedures document (65 pages plus Safety Data Sheets) has been prepared and submitted to the Environmental Heath and Safety (EH&S) of UTEP.
  This document is updated each time when a new procedure is added.

## Slide 8
Accomplishments and Progress
Magnesium borides were synthesized by two methods.
Combustion synthesis (chemical oven)
  A ceramic (BN) crucible with an Mg/B pellet surrounded by an annular layer of a Ti/B (1:2 mole ratio) mixture
  The crucible is placed into a chamber filled with Ar.
  The Ti/B mixture is ignited by a hot wire or by a laser.
  The released heat ignites the Mg/B mixture.
  Heating rate: 300-500°C/s
Laser ignition setup
Hot-wire ignition setup
Chemical oven schematic
Crucible
Ti/B mixture
Mg/B pellet

## Slide 9
Accomplishments and Progress
Tube furnace
  Mg/B pellet in Ar flow
  Heated at 5°C/min up to 650–1050°C.
  Held for 1 – 6 h.
  Cooled at a rate of 5°C/min.
Tube furnace

## Slide 10
Accomplishments and Progress
XRD patterns of MgB2 products synthesized by the chemical oven technique (left) and in a tube furnace (right)
MgO
MgB2
MgO
MgB2
Synthesis of MgB2
Heating at 750 °C for 2 h
Synthesis of MgB2
Chemical oven
MgB2
MgO
MgO
MgB2

## Slide 11
Accomplishments and Progress
The products were ground via surfactant-assisted ball milling in a SPEX shaker.
  Scanning electron microscopy shows nanoscale particles.
  Particle size analysis indicates agglomeration.
SEM image of milled MgB2
Particle size distribution of milled MgB2

## Slide 12
Accomplishments and Progress
XRD patterns of MgB4 (left) and MgB4-MgB7 (right) products synthesized in a tube furnace
80 at% B in the initial Mg/B mixture
MgO
MgB4
MgO
MgB7
Synthesis of MgB4
Heating at 1050°C for 1 h
Synthesis of MgB4-MgB7
Heating at 1050°C for 3 h
MgO
MgO
MgB7
MgB4

## Slide 13
Accomplishments and Progress
XRD patterns of MgB20 products synthesized by the chemical oven technique (left) and in a tube furnace (right) 91 at% B in the initial Mg/B mixture
MgO
MgO
MgB20
MgB20
Synthesis of MgB20
Heating at 1050°C for 2 h
Synthesis of MgB20
Chemical oven
MgO
MgO

## Slide 14
Accomplishments and Progress
Removal of MgO from the products by acid leaching
  The powder is submersed in nitric acid (1M) for 5 min.
  Nitric acid is removed by vacuum filtration followed by washing in ethanol, deionized water, and acetone.
XRD patterns of MgB4–containing products before (left) and after (right) acid leaching
MgO
MgB4
MgO
MgB4

## Slide 15
Accomplishments and Progress
Scanning electron microscopy shows that the leached MgB4 powder consists of irregularly shaped particles, approximately 1 µm in size.
SEM image of the leached MgB4 sample

## Slide 16
Accomplishments and Progress
Preventing MgO formation
  MgBx products synthesized with high-purity boron (min. 98% B) have less MgO than those synthesized with low-purity boron (93-96% B).
XRD patterns of MgB4 synthesized using low-purity (left) and high-purity (right) boron
MgO
MgB4
MgO
MgB4

## Slide 17
This project has not been previously reviewed at an AMR.
Accomplishments and Progress: Responses to Previous Year Reviewers’ Comments

## Slide 18
Collaboration and Coordination
Collaborator:
  Dr. Vitalie Stavila, Sandia National Laboratories – Livermore
The collaborator studies hydrogenation and dehydrogenation of the materials synthesized at UTEP using SNL facilities for pressure-composition-temperature (PCT) measurements and high-pressure hydrogenation.
Miguel Camarena visited SNL in the summer of 2023 and performed:
  Characterization of Mg-B materials (XRD and FTIR spectroscopy)
  Chemical purification of Mg-B materials
Andre Molina will be trained at SNL in summer 2024.

## Slide 19
DEIA/Community Benefits Plans and Activities
The project helps maintain and upgrade educational, training, and research capabilities of UTEP, a prominent minority-serving university.
  Over 24,000 students
  Most students are drawn from the Southwest border region with a population of over 80% Hispanics.
  A student body is 84% Hispanic.
  Approximately 50% of UTEP students are first in their families to attend college.
Two Mexican American students are directly involved in the project.
  Research at UTEP
  Training at Sandia National Laboratories – Livermore

## Slide 20
Remaining Challenges and Barriers
Fabrication and characterization of nanoscale/nanostructured MgBx (x≠2) materials remain a challenge.
Acid leaching does not remove MgO impurity completely.
Hydrogenation in a high-pressure differential scanning calorimeter has not shown any mass gain.
  MgB2 at 500 psi (34 bar) and 450°C for 5 h
  MgB4 at 1200 psi (83 bar) and 300°C for 5 h
High-pressure differential scanning calorimeter

## Slide 21
Proposed Future Work
Determine effective post-processing methods to create nanoscale or nanostructured MgBx materials.
Synthesize MgBx materials with x < 2.
Improve the MgO removal methods.
Continue to pass the obtained borides to the Collaborator for investigating their hydrogenation and dehydrogenation at Sandia National Laboratories.

## Slide 22
Summary
Four MgBx phases have been synthesized: MgB2, MgB4, MgB7, and MgB20.
The phase composition depends on the heating time.
Combustion synthesis cannot improve the product quality despite the very high heating rate; it also leads to loss of Mg.
An effective acid leaching procedure has been identified for removal of MgO.
Use of high-purity boron decreases the MgO impurity.
First samples have been shipped to the Collaborator for investigating their hydrogenation at Sandia National Laboratories.